## Slide 1: HGTD Cables and Connectors
Ricardo Gonçalo (LIP/Univ. Coimbra)

## Slide 2: Cables: from TileCal (General Cable)
Last version not good in fire test – needed to change insulation thickness
Two new prototypes are being produced – to be done this week or next
Circular section, unlike last one
Expected diameter 13.5– 14 mm

## Slide 3: Connectors
We have been using this one for Patch Panel development:
  http://www.farnell.com/datasheets/2916873.pdf
  Unit price (120 pins, small quant.): 53 € plug; 45 € pins; 26 € conector (old price)
  Good mechanical stability
Looks good for long-cable to
Patch Panel conneciton
REF:516-120-000-101 REF:516-056-000-301 REF:516-120-000-402 REF:516-056-000-402 REF:516-230-512 REF:516 230-556

## Slide 4: IDC Connectors – from Agostinho Gomes
CERN BE-EA Cabling Team suggested Insulation Displacement Crimping Connectors (IDC)
Found IDC connectors from TE suited for solid copper wires: https://pt.farnell.com/amp-te-connectivity/1-745495-8/socket-idc-d-metal-25way/dp/1098474?CMP=GRHB-OCTOPART https://www.farnell.com/datasheets/1639165.pdf
Tested the connectors
From the shelf their voltage limitation is low: sparks appear around 1.6 kV in any of the 2 rows, but not inter rows
Is it a problem? Neither for ground pins nor for HV pins (max voltage difference is 360 V), but it is a problem for pin 13 (drain wire) that has a neighbour at HV.

## Slide 5: IDC Connectors fix using Araldite epoxy
Weak point is a ~1 mm wide line where the pin to pin lateral insulation is cut/missing
Distance between sharp metallic contacts of the order of 0.5 mm, prone to generate sparks above 1.5 kV
After insertion of the wires, covering the contacts with Araldite epoxy provides excellent insulation between adjacent pins
Limit for sparks in the connector jumps to ~2.7 kV

## Slide 6: IDC Connectors with Araldite
First test with a “slow” epoxy
First test with a “5 min” fast araldite epoxy, only a thin transparent layer of epoxy
Araldite epoxy, thick layers after 2 applications
As a bonus, the epoxy strengthens the wire connections

## Slide 7: Bonus slides

## Slide 9: Patch Panel Grounding & Shielding
Use filter module boxes as continuation of vessel Faraday cage
  Also DC connecttion of filter boards backplane to cage
DC connection of Faraday cage to local TileCal earth
  DC current not as bad as HF AC noise
Move common-mode filter capacitors to filter input instead of output
  Filter common mode current at input

## Slide 10: Patch Panel Units Design
A modular design is proposed for the patch panels
Individual modules are aluminium boxes containing two filter boards and connectors
  Provide mechanical support and insulate each pair of boards within separate Faraday cage
  Easy to construct, handle and access for maintenance
  14 RC-RC low-pass filters in each filter board
  Means one 56-wire cable connected to each module: = 28 HV channels = 14 channels x 2 boards
  Routing of individual HV channels through wires connecting cables to each filter board

## Slide 11: Old prototype